Alignment of Flanges to Equipment

Content

1	Scope	3

2	Purpose	3

3	Definitions	3

4	Applicable Documents	3

5	Responsibility, Procedure	3

5.1	Responsibility	3

5.2	General Requirements	4

5.3	Alignment Methods	4

5.4	Tolerances for Connections to Equipment	5

6	Documentation and Records	5

# Scope

This specification applies for construction sites and defines adequate rectification methods and the workflow for the alignment of flanges to equipment.

# Purpose

The acceptable alignment of flanges to equipment shall be ensured by using approved methods. This specification determines minimum requirements for:

A		cutting and welding
B		grinding of existing butt weld to a certain extent and re-welding
C		flame straightening of piping

The Specification applies for construction sites including pre-fabrication yards.

# Definitions

| COMPANY | Linde LE |
| --- | --- |
| CONTRACTOR | The party which is awarded a contract from LE |
| Construction Site | Main term for fabrication sites for prefabrication or field assembly as well as existing plants where repair work or reconstruction is carried out. |
| NDT | Non Destructive Testing |
| NPS | Nominal Pipe Size |
| WPS/PQR | Welding Procedure Specification / Procedure Qualification Record |

# Applicable Documents

Equipment manufacturer's tolerances for flange alignments (shall govern).

LS 142-01			Flame Straightening of Piping

&CG-W-SC 9224 (EN)	Specification - Above Ground Piping Construction

&AA-W-QA 2402 (EN)		Flange Alignment - Acceptance Sheet

# Responsibility, Procedure

## Responsibility

The CONTRACTOR is responsible to ensure a stress free alignment of flanged connections.

CONTRACTOR’s personnel responsible for the alignment of flanges shall be skilled and thoroughly experienced.

Personnel shall be nominated to COMPANY in writing prior to start of alignment activities acc. to this specification.

## General Requirements

-	Alignments shall be made prior to pressure test.
-	Prior to alignment the piping section shall be disconnected from equipment.
-	Prior to alignment bolts and gaskets shall be removed from flanges.
-	A written request for approval with the proposed alignment method is required where one of the 	following specified tolerances is exceeded.

- Offset of centrelines

- Flange face parallelism

- Flange face distance

- Bolt Hole mismatch

The request shall contain the measured misalignment prior to rectification. A copy of the Isometric drawing shall be attached to the notification. The proposed alignment method shall be approved by COMPANY site management.

## Alignment Methods

Alignment may be performed by following methods (table 1)

A		Cutting and welding
B		Grinding of existing butt weld to a certain extent and depth, followed by re-welding
C		Flame straightening

Table 1

| Method | Material | Diameter Limitation | Wallthickness Limitation |
| --- | --- | --- | --- |
| A | All | No | No |
| B | All | No | No |
| C refer to LS 142-01 | C- und C-Mn-Steel with min. specified Yield Strengths ≤ 355 N/mm2, for specified min. Design Temp. ≥ -46 °C Austenitic CrNi-Steels | No | < 20 mm |

### Method A

This method shall be used preferably.

Welding Parameters
The applicable PQR and WPS shall be followed, including post weld heat treatment if applicable.

Spacing Pieces
In case of applying spacing pieces, the distance of circumferential welds shall not be less than
1 x NPS, however min. 50mm.

### Method B

This method requires thorough consideration.

Grinding
The partial removal of weld deposit depends on the existing misalignment and welding parameters.
Grinding and re-welding shall be performed minimum half of the circumference.

Welding Parameters / NDT
The specified PQR and WPS shall be followed, including post weld heat treatment if applicable.
The weld shall be subject to 100% radiography.

### Method C

Flame straightening on pipe lines requires a fundamental skill.

Linde Standard LS 142-01 shall be applied for Method C.

## Tolerances for Connections to Equipment

Tolerances as defined in table 2 are applicable unless more stringent tolerances are given by equipment manufacturer.

Table 2

| Max. permissible Tolerances for Connections to Equipment |  |
| --- | --- |
| Vertical and horizontal centreline offset | 0.8 mm |
| Bolt hole offset | 0,8 mm (bolts shall be freely movable) |
| Flange face parallelism (at outer face diam.) | NPS < 4" 0.4 mm NPS 4" – 8" 0.6 mm NPS > 8" 0.8 mm |
| Flange face distance | gasket thickness + 0,5 mm |

# Documentation and Records

Alignment methods A and B shall be documented in the Isometric Supplement Sheet, stating the relevant WPS and the welder no. If the weld was subject to non-destructive testing prior to alignment, the same method shall be repeated and documented after alignment.

Alignments performed on sensitive or rotating equipment for all methods shall be documented in addition on the Flange Alignment - Acceptance Sheet &AA-W-QA 2402 (EN).